Classic Handmade Roof Tiles



Handmade roof tiles with variations in texture and shape to give special character to the roof. Naturally coloured without the use of surface stains or coloured sands.

A range of matching handmade fittings in a sandfaced finish.

# Product Reference

# Classic

# Colours and Finishes

Staffs Blue

Dark Heather

Deep Red

Purple Brown

Bronze

**Options**

In addition to plain classic tiles, eaves and gables, there is a range of four ornamental tiles, usually used as feature courses. Shapes available are 'Arrowhead', 'Club', 'Fishtail' and 'Spade'.

**Guidance**

Size Classic 265 x 165mm  
Eaves 215 x 165mm  
Gables 265 x 248mm

Weight Classic 1.51kg  
Eaves 1.2kg  
Gables 2.3kg

Pattern Handmade

Material Etruria Marl

Minimum Pitch 35 degrees

Manufacturing Standard BS EN 1304

Quantity Guide @ 100mm gauge pitched roof 60/sq meter

@115mm gauge vertical tiling 53/sq meter

**Fixing Standards**BS 5534 Code of Practice for Slating and Tiling

BS 8000 part 6 Workmanship on Building Sites