Dreadnought Plain Clay Roof Tiles



A wide range of traditional plain clay roof tiles in a smoothfaced, sandfaced or rustic finish. The natural burnt clay colours are produced entirely by control of the kiln atmosphere and without the use of colouring agents. These colours are permanent and unaffected by exposure to UHV light.

# Colours and Finishes

Staffs Blue Smoothfaced, Sandfaced or Rustic

Dark Heather Sandfaced or Rustic

Blue Brindle Smoothfaced

Brown Antique Smoothfaced, Sandfaced or Rustic

Brown Heather Sandfaced or Rustic

Brown Brindle Smoothfaced

Country Brown Smoothfaced, Sandfaced or Rustic

Red Blue Blend Smoothfaced, Sandfaced or Rustic

Red Smoothfaced, Sandfaced or Rustic

Plum Red Smoothfaced

Mixed tiles: Dreadnought’s naturally coloured tiles can be mixed to produce a blended roof

Collingwood Blend Smoothfaced, Sandfaced or Rustic   
70% Brown Briindle/Brown Heather and 30% Country Brown

Trafalgar Blend Smoothfaced, Sandfaced or Rustic  
33% Brown Briindle/Brown Heather and 33% Country Brown 33% Brown Antique  
**Consult with Dreadnought Tiles for other recommendations.**

**Options**

In addition to plain tiles, eaves and gables, there is a range of four ornamental tiles, usually used as feature courses. Shapes available are 'Arrowhead', 'Club', 'Fishtail' and 'Spade'.

**Guidance**

Size Machine made, rustic and ornamental tiles 265 x 165mm  
Eaves 215 x 165mm  
Gables 265 x 248mm

Weight Machine made and rustic tiles 1.19kg  
Eaves 0.95kg  
Gables 1.8kg

Pattern Traditional single camber machine made, or single camber rustic

Material Etruria Marl

Minimum Pitch 35 degrees

Manufacturing Standard BS EN 1304

Quantity Guide @ 100mm gauge pitched roof 60/m2

@115mm gauge vertical tiling 53/ m2

**Fixing Standards**BS 5534 Code of Practice for Slating and Tiling

BS 8000 part 6 Workmanship on Building Sites