## STRUCTURAL EPOXY BRICK SLIP ADHESIVE

## S - 2625 E

# OVERVIEW

Manufactured by Structural Adhesives Ltd, S-2625 E should be used where there are no issues with movement or differential expansion.  This Epoxy based adhesive is a 2 part formulation which delivers greater strength than other adhesive types but is brittle so should not be used where movement can occur.  Care must be taken when handling and using all epoxy based adhesives and reference must be made to the COSH information.

# DESCRIPTION

S-2625 E is a two part, cold curing epoxy adhesive.  It is designed to bond brick to brick in cut and bond applications and brick slips to various substrates such as existing brick work, concrete, cement board, ply wood, exposed aggregate, stainless steel and Aluminium. Its rapid rate of cure enables work to be moved after about 4 hours.

# INSTRUCTIONS

Refer to the Material Safety Data Sheet before use. Mix part 1 and Part 2 in equal quantities by weight or volume.  Make sure the adhesive is mixed thoroughly before applying.  Apply the adhesive to one surface and immediately bring the surfaces together to form a bond.  When bonding brick slips the adhesive should be applied with a serrated trowel to the bonding surface and the brick slips pressed onto the adhesive. Use 10mm spacers to give the appearance of 10mm joints which can be filled in with S – 2382E.

# TYPICAL PROPERTIES

|  | Part 1 | Part 2 | Mix |
| --- | --- | --- | --- |
| Appearance | Various colour | Natural |  |
| Consistency | Thixotropic paste | Thixotropic paste |  |
| SG | 1.45 | 1.47 |  |
| Mix ratio |  |  | 1:1 |
| Work-life, bead |  |  | 45 min |
| Shear strength, 1 day steel |  |  | 2350 psi |
| Stainless steel, 1 day |  |  | 1845 psi |
| Aluminium |  |  | 1731 psi |
| Zintec |  |  | 1700 psi |
| Timber |  |  | 1025 psi |
| GRP |  |  | 457 psi |
| Bond strength, brick |  |  | Brick/ brick failure |
| Compression (12.5mm plug) |  |  | 57 Nmm-² |

# FREEZE/THAW TEST

A brick slip panel using this material as the adhesive for bonding the slips, has been tested by an independent laboratory in accordance with section 5.1 of BS 3921:1985. The panel withstood 100 cycles without any defect and has been classified as frost resistant.

# FLEXURAL BEND TEST

A three-point flexural bend test was performed on a 2.5m steel lintel with brick slips stuck to it using S-2625E as the adhesive.  The beam was loaded to 27kN to a deflection of 2.38 mm with no loss of brick slips and no adhesive failure.

# APPLICATION

| Coverage | When applied using a serrated trowel allowing a 1.5mm glue-line, allow approximately 2.2kg/ m²(60 standard sized brick slips). |
| --- | --- |
| Application Temperature | +5°C to + 30°C |

# STORAGE

Store between 5 and 25°C.

# SHELF LIFE

12 months in above conditions of storage.

# PACKAGING

Available in 12kg and 50kg packs.  As a guide a 12kg pack will cover 5.5m2

# WORKING SAFELY WITH EPOXIES

Please read this guide prior to working with epoxy resins. Read thoroughly all Material Safety Data Sheets (MSDS) and follow product labels and warnings.

Epoxies pose a chronic health risk due to overexposure by skin, inhalation, or ingestion. Your body’s reaction to overexposure is called sensitization. This means that even small doses of repeated direct contact with skin can eventually make someone allergic to the resin itself, causing anything from a small skin rash to a more systemic allergic response requiring medical attention. Susceptibility to epoxy sensitization varies amongst individuals. Therefore the best way to prevent sensitization problems is to limit exposure. Even dust from cured epoxy can be sensitizing.

Skin Contact is the most common means of exposure to resins. Even repetitive minor skin contact can cause chronic sensitization symptoms. Avoid contact with resin, hardeners, mixed epoxy and cured sanding dust from epoxy. Wear protective gloves and clothing whenever you handle epoxies. Barrier skin creams provide supplementary protection. If you do get resin, hardener or mixed epoxy on your skin, remove it as soon as possible. Use oil-based or citrus skin cleaners to remove resin or mixed epoxy from your skin followed by soap and warm water. Always wash thoroughly with soap and warm water after using epoxy, removing amine blush or sanding epoxy from your skin. If you spill epoxy on your clothes, change them immediately. Use skin cleanser to remove any epoxy from you and your clothes. If you cannot completely remove it from your clothes, do not continue to wear them. Never use solvents to remove epoxy from your skin. Stop using the product if you develop a reaction. Resume work only after the symptoms disappear, usually after several days. When you resume work, improve your safety precautions to prevent exposure to epoxy, its vapors and sanding dust. If problems persist, discontinue use and consult a physician. Protect your eyes from contact with resin, hardeners, mixed epoxy, and sanding dust by wearing appropriate eye protection. If epoxy gets in your eyes, immediately flush them with water under low pressure for 15 minutes. If discomfort persists, seek medical attention.

Keep your workshop clean to avoid incidental contact. Avoid touching door handles, light switches and containers when you have epoxy residue on your gloves, as this is a common source of sensitization. This can also cause sensitization to other members of staff who may not wear gloves such as office staff.

# NOTE

This disclaimer is issued by Structural Adhesives Limited ("the Company") and applies to the use of any products supplied by the Company ("the Products") displayed on this Technical Data Sheet (“TDS”). Please read this disclaimer carefully before using any of the Products. While the information and recommendations in this publication are to the best of our knowledge, information and belief, accurate at the date of publication, Structural Adhesives Ltd MAKES NO WARRANTIES, EXPRESSED OR IMPLIED OR OTHERWISE.  IN ALL CASES THE USER IS RESPONSIBLE FOR DETERMINING WHETHER THE STRUCTURAL ADHESIVE LTD PRODUCT IS FIT FOR A PARTICULAR PURPOSE AND SUITABLE FOR USER'S METHOD OF USE OR APPLICATION. THE PRODUCT MAY PRESENT HAZARDS AND SHOULD BE USED WITH CAUTION.  WHILE CERTAIN HAZARDS ARE DESCRIBED IN THIS PUBLICATION, NO GUARANTEE IS MADE THAT THESE ARE THE ONLY HAZARDS THAT EXIST.  Hazards, toxicity and behaviour of the products may differ when used with other materials and are dependent upon the manufacturing circumstances or other processes.  It is essential that the user evaluate hazards, toxicity and behaviour and this information be made available to processors, handlers and end users.

Using this TDS and/or the product constitutes your acceptance of this disclaimer.  This TDS covers just one of a large range of products supplied by Structural Adhesives Ltd.

Full information on these products and advice on application is freely available from our fully trained technical team. However NO PERSON OR ORGANISATION EXCEPT A DULY AUTHORISED STRUCTURAL ADHESIVES LTD EMPLOYEE IS AUTHORISED TO MAKE AVAILABLE DATA SHEETS FOR STRUCTURAL ADHESIVES LTD PRODUCTS.  DATA SHEETS FROM UNAUTHORISED SOURCES MAY CONTAIN INFORMATION THAT IS NO LONGER CURRENT OR ACCURATE.

This TDS supersedes all previous TDS’s relating to the products, and users of it must ensure that it is the current issue. Destroy all previous TDS’s, and if in any doubt, contact Structural Adhesives Ltd quoting the product and data sheet number.

No part of this data sheet can be reproduced or transmitted in any form, or by any means without prior written consent from Structural Adhesives Ltd.

This product is further sold subject to the Company's Conditions of Sale, which are made available to the customer prior to an order being accepted.